Construction

- Central strength member: Glass reinforced plastic (GRP) rod - Buffer tubes: Dry 2.5 mm polypropylene tube, 12 fibers per tube - Optical fibers: 144 Corning SMF28e+ ITU.G652.D single mode fibers - Water tightness: Longitudinal water tightness is ensured with dry blocking material - Reinforcement: Dielectric strength yarns over core - Outer jacket: 1.3 mm nominal black weather resistant medium density polyethylene

Dimensions

| Fiber Count | ## 144 |
| --- | --- |
| Outer Diameter | 0.63 in (15.9 mm) |
| Weight | 105 lb/kft (156 kg/km) |

Main mechanical and environmental properties

Complies with the requirements of Telcordia GR-20-CORE, RUS 7 CFR 1755.900 and ICEA 640.

Mechanical properties

| Minimum bending radius – under tension – no tension Installation Tension | 20 x cable diameter 10 x cable diameter 600 lbs max | Temperature range – transportation, storage – installation - operation | -40°C to +75°C -30°C to +70°C -40°C to +70°C |
| --- | --- | --- | --- |

| Test | Standard | Specified value | Acceptance criteria |
| --- | --- | --- | --- |
| Temperature cycling | Telcordia GR-20 | -40°C to +70°C | GR-20 : R6-69 |
| Water penetration | Telcordia GR-20 | Sample=1m, water=1m, 24h | GR-20 : R6-75 |

Marking

Except where expressly agreed between the parties and specified to the contrary at the time the order is made, all cable markings shall be in white or yellow, at two foot or one meter intervals on the outer jacket, and shall include the following inscriptions:

(handset symbol), PRYSMIAN OPTICAL CABLE, month/year of manufacture, number and type of fibers, cable ID number, length marking